## Slide 1: Shielded Metal Arc Welding
Part II
General Information
Polarity
Set Up
Striking an Arc

## Slide 2: Shielded Metal Arc Welding
An arc welding process with an arc between a covered
electrode and the weld pool. The process is used with
shielding from the decomposition of the electrode
covering,
without the
application of
pressure
and with filler
metal from
the electrode.

## Slide 3: Principles of the SMAW Process
Electric Arc Between Electrode & Work, Melts the Electrode & Fuses the Joint
Weld Metal & Slag Form
Slag is Lighter than the Molten Metal & Rises to the Top
AC or DC Polarity
Notes: The arc melts the electrode and base material in the immediate area, and any metalic particles that may be in the electrode covering.
The arc zone is filled with a shielding gas produced by the burning flux coating which protects the molten metal from contaminants (oxygen and nitrogen).
The resultant weld bead has a protective slag covering that needs to be removed. The weld bead appearance is dependant upon the welding technique used; either a whip or a drag technique. The technique used depends on the electrode used and the welding application.
SMAW polarity depends on the electrode selection, which depends on the application.

## Slide 4: DCEN (Striaght) Polarity
DC -
Heat Concentrated at Electrode
Lower Penetration
Increased Deposition Rates
Notes: All three welding polarities are used in SMAW welding. Electrode polarity in shielded metal arc welding is determined by the electrode coating as well as the desired weld bead.
Welding polarity in SMAW is highly dependent upon the type of electrode being used and the application. Direct Current Electrode Negative is also used in SMAW welding. It is sometimes used for the Fill-Freeze electrode group. These electrodes will be discussed thoroughly later in the program.
DC- polarity in SMAW welding can be easily defined in terms of the direction that ions flow as well as where the heat of the arc is directed.
Ions are emitted from the work piece to the electrode and electrons flow in the opposite direction. DC- polarity is a shallow penetrating polarity because the majority of the heat of the arc is concentrated on the electrode and not the work piece.
DC- polarity often is most commonly used for applications requiring fast travel speeds on sheet metal.

## Slide 5: Direct Current Electrode Negative
DCEN
Direct Current Electrode Negative (DCEN):The
arrangement of direct current arc welding
cables/leads in which the electrode is the
negative pole and the workpiece is the positive pole
of the welding arc.
Notes: In order to change the AC input power to produce DC welding output, a device must be present in the power supply.
This device is called a rectifier. A rectifier allows current to flow in one direction only.
The direction of the current flow determines the DC polarity.
The choices are DC+ or DC-.
DC- or direct current electrode negative is the arrangement of direct current arc welding cables/leads in which the electrode is the negative pole and the workpiece is the positive pole of the welding arc.
When using DC- polarity in SMAW welding, the majority of the heat is directed at the electrode. The electrodes designed for DC- polarity produce weld deposits with shallow penetration. Primary applications are fast travel speeds on sheet metal.

## Slide 6: DCEP (Reverse) Polarity
DC +
Heat Concentrated at Workpiece
Forceful, Digging Arc
Medium to Deep Penetration
Notes: All three welding polarities are used in SMAW welding. Electrode polarity in shielded metal arc welding is determined by the electrode coating as well as the desired weld bead.
The majority of SMAW welding is done using direct current electrode positive polarity. Also, the majority of stick electrodes are designed to operate using this polarity as either the primary polarity or as a secondary polarity.
DC+ polarity in shielded metal arc welding also can be easily defined in terms of the direction that ions flow where the heat of the arc is directed.
DC+ is just the opposite of DC- polarity. Ions are emitted from the electrode to the work piece and electrons are emitted from the work piece to the electrode.
In this condition, the majority of the heat is concentrated at the work piece, resulting in a deep, penetrating weld bead. DC+ polarity is the primary polarity for the Fast Freeze electrode group and the majority of the electrodes found in the Low Hydrogen group.

## Slide 7: Direct Current Electrode Positive
DCEP
Direct Current Electrode Positive (DCEP): The
arrangement of direct current arc welding
cables/leads in which the electrode is the
positive pole and the workpiece is the negative pole
of the welding arc.
Notes: DC+ or direct current electrode positive is the opposite of DC- or direct current electrode negative. In this case, the electrode is the positive pole and the workpiece is the negative pole.
When using DC+ polarity in SMAW welding, the majority of the heat is directed at the work piece. The electrodes designed for DC+ polarity produce weld deposits with deep penetration. Primary applications are for pipe welding, general purpose and maintenance welding, deep penetration applications, and on base material with surface contaminants.

## Slide 8: AC Polarity
Medium Penetration
Medium Travel Speeds
Notes: <number>
<header>
Alternating current or AC polarity is a mixture of DC+ and DC- polarity. The desirable features of both other modes are obtained to a reduced level. 50% of the time, ions are emitted from the electrode and 50% of the time, ions are emitted from the work piece. This 50/50 mix results in medium penetration levels and medium travel speeds.
Think of AC as being electrode positive for 50% of the time or half of the cycle, and electrode negative for 50% of the time or the other half of a cycle. AC polarity is used as the primary polarity for the fast-fill electrode group. This is because these electrodes perform better on AC, and higher amperages can be used on AC than the DC polarities. Using higher amperages results in higher deposition rates. This is the main advantage of the electrodes in the Fast-Fill group; high deposition rates. Fast-Fill electrodes contain iron powder in their coatings that add to the weld deposit. This iron powder requires higher amperages to be used to properly melt the electrode. The higher amperage used then corresponds with higher deposit rates.
AC polarity is also used as the welding polarity to reduce the chance of having arc blow problems. Arc blow is a phenomenon that occurs when an electric arc is deflected from its normal path because of magnetic forces. When using AC polarity, the direction of magnetic forces occurs so rapidly (120 times a second), arc blow limitations are greatly reduced. Many Lincoln Electric electrodes are multi-polarity electrodes that permit operation on DC and AC polarity.
There are also shielded metal arc welding power sources that only provide AC welding output. This is another need/application for this polarity.

## Slide 9: Alternating Current
Alternating Current (AC): A current which reverses
at regularly recurring intervals of time (every 1/100 or
1/120 of a second) and which has alternately positive
and negative values. Modern power systems normally
generate a sinusoidal alternating current of either 50
or 60 Hertz (Hz).
Notes: Alternating current is a current that reverses regularly in recurring intervals of time 1/120th (60Hz) of a second.
AC is the type of power used in the United States as the standard for input power to run any electrical equipment or apparatus. It has alternating positive and negative values. In other words, it switches from DC+ to DC-, and it switches back and forth very rapidly.
The picture shown is an AC sine wave and the frequency of current flow through one sine wave is 60 Hz or 60 times a second in the U.S.

## Slide 10: Lincoln Equipment Setup
On/Off Switch
Electrode Lead
Work Clamp
Work Lead
Amperage Dial
Electrode Holder
Amperage Indicator
Polarity Switch
Idealarc 250
Notes: The components needed for a complete SMAW setup include: A constant current power supply. A constant current power supply maintains a preset amperage even for changes in arc voltage. In the case of constant current welding, arc voltage is determined from arc length, which is the distance from the end of the electrode to the work piece. Continuing to complete a SMAW welding package, an electrode holder is needed. The electrode holder is chosen based on the amperage being used to weld. Remember that electrode holders are rated according to their current capacities. The length and size of the electrode cable is also very dependent upon the amperage being used. The longer the length of cable being used for welding far distances from the power supply, the larger the cable needed. There are easy to follow charts available to properly size cables. Proper construction and size of the cable are important to efficient welding. The end of the cable opposite the electrode holder needs to be connected to the proper electrical connection on the power supply. There are two styles of connections: lugged connections and quick disconnects (QDs or TWIST-MATES). In the photo, the power supply has lugged cable connections.A work cable and clamp are also needed to complete the set up of a SMAW welding package. A work clamp is also selected according to the amperage being used for welding. They come in various sizes and amperage ratings. A work clamp is bolted to the lug at the end of the work cable, and the opposite end of this cable will be attached to the opposite connection on the power supply than the electrode holder.When connecting the electrode holder and the work cable and clamp to the power supply, care must be taken to connect these cables to the correct connection for proper welding polarity. Power supplies are either marked “+” and “-“ or “to electrode” and “to work” at the output connections. Electrode polarity is determined where the electrode holder and cable is connected. For example, for DC+ (direct current electrode positive) polarity, the electrode holder and cable would be connected to the output connector marked “+” and the work connection to “-“ in the first style of power supply. In the second style of power supply, there will be a polarity switch to determine welding polarity, and the appropriate cable will be connected to the similarly marked output connector. In Shielded Metal Arc Welding, all polarities are used. Welding polarity is determined by the electrode being used and the application.In the photo, there is a complete set up of a Lincoln Electric IDEALARC 250. This power supply is marked “to electrode” and “to work” at the output connections, and there is a polarity switch on the power supply. It is an AC/DC power supply and can weld the majority of SMAW electrodes.On the front of this power supply, there is a circular knob that controls amperage along with a dial with an indicator to point at the amperage setting. There are two amperage ranges in which the dial points: one for AC polarity and one for DC. The amperage range of this power supply is 50-315 amps and amperage is set according to the size and type of electrode being used, which is determined by the welding application. In constant current welding, voltage is never set, but is determined by the operator’s arc length.Once the equipment is set up properly and the amperage and polarity are set, welding begins by connecting the work cable to the work piece being welded (or to a grounded part) and by “striking” the SMAW electrode on the piece being welded. This completes the electrical circuit and the electrode and base material melt and weld together.

## Slide 11: Lincoln Equipment Setup
Electrode Cable
Electrode Jaw
Upper Jaw Insulation
Lower Jaw
Arm Insulation
Cable Coupling
Grip Handle
Connector Pin
Lower Jaw Insulation
Magnum 300 Amp Electrode Holder
Notes: The first criteria when deciding upon the proper SMAW electrode holder to use should be the amperage or amperages with which you are welding.
After determining the application and the amperage to use, the electrode holder is chosen and then the proper electrode for the application is chosen.
Electrode cables come in various lengths. The cable should be as short as possible for the application. This helps to prevent coiling or cluttering of the workspace with cumbersome cables. Cable sizes are chosen by welding amperage and length of cable.

## Slide 12: SMAW - Lincoln Equipment Setup
GC 300
Tighten Lug To Ground Clamp
Secure Lug to Cable
Magnum 300 Amp Work Clamp
Notes: The work cable lug must be securely connected to the work clamp.The first criteria to use when deciding upon the proper SMAW work clamp should be the amperage being run as they are also rated according to welding amperage. The work cable is lugged and attached to the work piece.The cable should be as short as possible for the application. This helps to prevent coiling or cluttering of the workspace with cumbersome cables.The photo shown is a GC 300 work clamp. However, all work clamps are similar in nature.

## Slide 13: Lincoln Equipment Setup
Notes: This slide shows a common SMAW setup.
Optional setup configurations have the power source mounted on an undercarriage so that it is portable and can be moved around the shop.
An electrode holder, work clamp and connecting cables complete the setup.
General setup procedures include:
  Verify that the welding machine is a constant current power supply.
  Check to be sure that the welding machine is properly grounded through the primary current receptacle, and that the machine is set up for the correct input voltage.
  Verify the location of the primary current disconnect.
  Locate the SMAW electrode holder and cable assembly.
  Set up the welding machine for the correct polarity DCEP (Direct Current Electrode Positive), DCEN (Direct Current Electrode Negative) or for AC.
  Choose the best electrode for the application.
  Set current based upon the electrode size and application.

## Slide 14: Shielded Metal Arc Welding
Known as Stick or Manual Welding
Uses CC Power Source
Versatile Process
All Polarities
Match Electrode with Power Source, Base Metal, and Joint Design
Notes: SMAW stands for shielded metal arc welding. It is often called stick welding or manual welding.
A constant current power supply is used.
It is possible to weld on both non-ferrous and ferrous materials with the shielded metal arc process, and produce x-ray quality welds, while using a consumable flux-coated electrode.
Shielded metal arc welding is done with DC+, DC- or AC current. Electrode polarity is highly dependent on the electrode and welding application.

## Slide 15: The SMAW Process Basics
Arc
Original Surface Of Base Metal
Reinforcement-
Build-up of
Weld Metal
Slag
Molten
Weld Metal
Protective Gas from Electrode Coating
Electrode Wire
(Filler Metal)
Electrode Coating (Flux)
Metal Droplets
Penetration
Arc
Notes: Shielded metal arc welding is a process in which the electric arc is transferred to the work piece through a flux-coated consumable electrode. SMAW is often called stick welding or manual welding. In this process, an electric arc is struck between the electrically grounded work and a 9-18” length of covered metal rod called the electrode. The electrode is clamped in an electrode holder, which is joined by a cable to the power supply. The welder grips the insulated handle of the electrode holder and maneuvers the tip of the electrode in respect to the welding joint. When the tip of the electrode touches the work, the electrical circuit is complete, and welding can commence. The heat of the arc melts the base metal, the electrode’s metal core and any metallic particles in the electrode coating. It also melts, vaporizes or breaks down chemically non-metallic substances in the coating for arc shielding, and/or for the addition of physical or mechanical properties.
The power source used is constant current.
A drag angle is recommended for SMAW to use the force of the arc to stay ahead of the puddle. This prevents the electrode from sticking into the puddle and the electrode coating from forming a slag inside the weld bead. This is called a slag inclusion and is a weld defect, and will need to be removed to prevent premature weld failure.
All welding polarities are used and are dependent upon the electrode being used and the application.

## Slide 16: Approximate Amperage Settings
Notes: Approximate electrode amperages can be set according to recommendations in electrode amperage charts.
The coatings on the four different groups of electrodes also have an effect on the current settings. “Fast freeze” type electrodes or organic will be on the low end of the range current because the current melts the core wire and there is a light coating on the electrode. “Fast fill” electrodes with 50% iron powder have a thick coating on the electrode and they will be on the high end of the current range because it will take more heat to efficiently melt the coating and the core wire.
When determining electrode amperages, be sure to consider:
  Position of the weld.
  Thickness of the weld metal.
  The type of joint being fabricated.
  Diameter of core wire will be another variable to consider - when determining electrode amperages.
  The polarity will determine the actual amperage setting.

## Slide 17: Starting The Arc
Scratch Start
Strike (Tap) Start
Notes: When starting the arc, strike the electrode like a match on the work surface by gently and quickly moving it along the weld metal.
Next, withdraw the electrode to form an arc length from the work piece of approximately 1/8”.
Reduce the arc length to the approximate length required to produce the desired weld.

## Slide 18: Restarting Interrupted Bead
1. Strike Arc Here
2. Move Electrode to Crown of Crater
3. Resume Travel Forward
Notes: To restart an interrupted weld bead, clean the previous crater of all slag.
To reinitiate the arc, strike ahead of the crater.
Once the arc has been struck, move back to the center of the weld crater and begin forward motion.

## Slide 19: Bead Initiation
Notes: In stick welding, more-so than all other arc welding processes, bead initiation or starting the arc is the most difficult. This is because the metal core of the electrode is conductive and most electrode coatings are not or some electrode coatings only have a small percentage of conductive materials in them.
In SMAW, bead initiation must be done with care. To do so, the electrode is lightly “struck” on the work piece and then removed within approximately ¼” from the work piece to keep the arc established. This action is very similar to striking a match. Care must be taken NOT to hit the electrode too hard on the work-piece, otherwise the electrode will stick to it. Also, care must be taken NOT to remove the electrode too far from the work piece after the initial strike. If the electrode is moved too far away, the arc will extinguish.
If it is extinguished, the entire process can be repeated by striking the electrode on the work piece. In some cases, when a stick electrode “sticks” to the work piece, it is sometimes difficult to remove, and upon removal some of the coating is also removed, preventing arc shielding and arc stabilization.
Also, when discussing the different groups of electrodes, some electrodes are better at arc starting and bead initiation than others. The electrodes with a percentage of iron powder in the coating tend to start better. This is because iron is conductive. Therefore, the metal core and the iron powder in the coating conduct electricity and help one another in arc starting.

## Slide 20: Bead Formation
Notes: Stringer beads involve moving the electrode along in a straight line down the welding joint as opposed to any weave motion. The end result is a flat smooth weld bead.
Some electrodes, primarily the Fast-Freeze group require a whip technique when welding a single pass weld, or on the first pass of a multiple pass weld.
Whipping the electrode involves starting the arc and creating a circle of molten weld metal at the beginning of welding. The electrode then is taken slightly out of the weld puddle momentarily, and then brought back into the center of the weld puddle. This action is repeated over and over again.
Whipping the electrode for this electrode group allows the weld puddle to freeze while the electrode is removed and then become molten again, as it returns. The end result of these welds is a rippled weld bead that resembles a roll of dimes.
Multiple passes are treated differently than the first pass. This is because the first pass must be completely covered and subsequent passes will increase the size of the weld. Multiple passes are generally done using a weave technique, but they may also be done using a stringer technique. There are many weave techniques that include side to side weaves, triangular weaves and box weaves.
The type and style of weave is operator preference and can be dependent upon joint design or application.
When weaving, care must be taken so that there is no weld bead undercut or gouging of the sides of the weld where inadequate fill of weld metal takes place. To prevent undercut, when at the sides of the weave, a slight hesitation of a second or so should take place to ensure proper fill of the sides of the weld and to prevent undercut.
Undercut is a visual defect, but can also cause cracking and other premature weld failures.

## Slide 21: Electrode Movement

## Slide 22: Electrode Movements

## Slide 23: Bead Termination
Notes: Welding termination in shielded metal arc welding is less critical than in other welding applications. However, in some cases, extra care is needed to prevent potential problems. In SMAW, the welding arc can be terminated simply by pulling the electrode away from the work-piece, and thus extinguishing the arc.
In some cases, this is not good enough. In these cases, if the bead is not terminated properly, a crater will possibly form at the end of the weld.
That crater because of its geometry being concave, is subject to cracks called “crater cracks”. It also has just a poor-finished look.
To prevent crater cracks, a common practice is to do something similar to a back-step (e.g., moving back over the last few inches of a weld to end the crater on top of a previously welded section and prevent crater crack).
This fills up before terminating the weld. Crater cracks can occur in all base materials
By holding the electrode at the crater long enough to let the metal solidify, a weld may be successfully terminated.
Another technique to prevent a large crater and potential crater crack is to use a run-off tab. Run-off tabs are small tacked pieces of metal that are at the end of the weld joint. Welding ends on these pieces rather than in the weld joint. Therefore, the crater is now on this tacked piece of material which is sawed or broken off and discarded.

## Slide 24: Sample Beads For Quality Welding
Notes: First bead on left Shows proper current, travel speed and arc length.
  Current is correct as the weld bead shows a bright silver color . Arc length is correct since the appropriate amount of penetration has been achieved. Travel speed is correct as the weld bead shows half moon or crescent shaped ripples. Travel angle is correct as the weld bead ripples show appropriate solidification. Work angle is correct as the weld bead ripples show the center of the ripple in the middle of the weld bead.
Second bead from leftShows what occurs when the current is too low.
  The weld bead shows shallow penetration. The weld bead is narrower than desired. The weld bead has a “mounded” crown and has a ropey appearance.
Third bead from leftShows when current is too high.
  There is a long, deep crater. The weld bead is abnormally wide. There will be excessive spatter because of excessive current.
Center bead Shows a short arc length.
  The weld bead shows shallow penetration. The weld bead is narrower than desired. The bead tends to have a ropey shape. There can be a chance of excessive spatter. There is a possibility of some porosity.
Third bead from rightShows a long arc length.
  The weld bead shows a wider than normal width because of the excessive distance between the electrode and the work-piece. The finished crater is deeper than necessary. The weld bead will have excessive spatter because of the excessive distance between the electrode and the work-piece.
Second bead from right Shows too slow of a travel speed.
  The weld bead is excessively wide. The weld bead has a “mounded” crown showing excessive deposition. The weld bead ripples will be very flat with little curvature to the ripple shape. The base plate should show an excessive amount of heat input.
First bead from rightShows too fast of a travel speed
  The weld bead is very narrow with little weld metal deposition. There can be some undercut on both sides of the weld bead. The finished crater will be shallower and narrower than normal.