## Slide 1: Shielded Metal Arc Welding
SMAW
Equipment
&
Safety
Notes: 1

## Slide 2
What is SMAW?
SMAW = Shielded Metal Arc Welding
“Stick” Welding or “Manual” Welding
Metal Rod Covered with Flux that Provides Shielding to Protect
the Weld
Uses Constant
Current Power
Sources
Most Widely Used Arc Welding Process in the World

## Slide 3: Power Supply
Must maintain a constant current (CC) with only a slight change in voltage
Varying voltage and current will result in a uneven arc
  Creates splatters & uneven welds
Three types of Power Supplies
  Generator (Portable Welder)
    Produces low voltage, high amperage current (D/C)
    Expensive to purchase & operate
  Transformer (Buzz Box)
    Change high voltage, low amperage current (A/C), to low voltage, high amperage current (A/C)
    Cheapest to purchase & operate
  Rectifier
    Allows electricity to flow in one direction only (D/C)
Notes: 3

## Slide 4
SMAW - Power Sources

## Slide 5: Constant Current
Welding Circuit Consists of Power Source, Electrode and Work Cables/Leads
The Power Source Keeps the Current as Constant as Possible even when the Operator Varies the Arc Length
Voltage is Proportional to Arc Length
Notes: 4

## Slide 6: Duty Cycle
The Duty Cycle of a power source is the percentage of a ten (10) minute period that it can operate at the rated output current setting.

## Slide 7: Duty Cycle
Duty Cycle Amperes Time
Available
30% 250 3 Min/10 Min
40% 225 4 Min/10 Min
50% 200 5 Min/10 Min
60% 190 6 Min/10 Min
70% 180 7 Min/10 Min
80% 170 8 Min/10 Min
90% 155 9 Min/10 Min
100% 140 10 Min/10 Min

## Slide 8: Ground Clamp & Electrode Holder
5. Ground Clamp
  Completes the full electrical circuit
  Must be fastened securely to the base metal or to the bench (metal) you are working on
  A bad connection will result in resistance build-up in the cables and connections
  Resistance generates heat which can damage and/or melt parts
6. Electrode Holder
  The stinger receives the amperage and directs it through the electrode to form the arc
  Should be well insulated & have a strong spring to hold the electrodes.
Notes: 13

## Slide 9: Cables
Allows the ground clamp and stinger to be mobile
Should be well insulated and protected from heat

## Slide 10: Electrode
Consists of a metal core coated with flux which shields the weld as it burns.
There are several types and sizes for different thicknesses and types of metal.

## Slide 11: Safety
Protective Clothing
Must be worn at all times when welding. The heat created during arc welding creates flying molten sparks and ultraviolet and infrared rays that can burn the skin.

## Slide 12: Protective Clothing (cont)
  Leather Gloves
    Gloves protect the hands from burns during welding.
    Should be made of thick leather and have long cuffs to protect the wrist area from sparks and heat.
  b. Sleeves
    A nonflammable material must be worn on the arms to protect from burns, sparks, and ultraviolet light.
Leather Cape
Sleeves/Bib
Leather Welding
Jacket
Leather Welding
Gloves

## Slide 13: Protective Clothing (cont)
Body Protection
  Leather clothing items are the best protection from heat and sparks. For light welding operations, coveralls work best but a work shirt will protect the body during arc welding.
  Protective clothing should fit properly and be free of rips or other openings through which sparks can enter.
Footwear
  Leather boots should be worn while welding
Leather Welding
Trousers
Leather Welding Apron

## Slide 14: Protective Clothing (cont)
Eye Protection
  The brilliant light given off by the electric arc produces invisible ultraviolet and infrared rays which can severely burn the eyes and skin. NEVER LOOK AT THE ARC WITH THE NAKED EYE!
  Welding Helmet
    Fits on the head using a plastic adjustable headband.
    This leaves both hands free to weld and position materials.
    Helmets have a clear cover lens to protect the filter lens and some have a clear lens underneath so the welder can chip slag.

## Slide 15: Protective Clothing (cont)
Protective Lenses
  Different types of welding use different amounts of voltage and current which determine the intensity of light and the amount of ultraviolet and infrared rays produced. Lens shades range from #5 (least protection) to #14 (most protection).
  1) Shade 5 Light spot welding
  2) Shade 6&7 Up to 30 amps
  3) Shade 8 30 - 70 amps
  4) Shade 10 75 - 200 amps
  5) Shade 12 200 - 400 amps
  Shade 14 over 400 amps
Cover Lenses
  Used to stop flying slag or metal which protects the filter lens
    Clear, unbreakable plastic is cheapest and lasts longest.

## Slide 16: Additional Safety Equipment
  Care of Lenses
    Must be changed if a crack or chip is found
    Periodic cleaning with soap and water is helpful
Additional Welding Equipment
  Tongs/Pliers
    The heat of the arc will transmit to the metal being welded. Use pliers or tongs to grab or move hot metal.
  Chipping Hammer
    Used to remove slag from the weld
  Steel Brush
    Used to clean the weld if a second pass is going to be made.